Supplementary Information for

Energy Breakdown in Capacitive Deionization

Ali Hemmatifar a, James W. Palko a, Michael Stadermann b , Juan G. Santiago a,

a Department of Mechanical Engineering, Stanford University, Stanford, California 94305, United States

b Lawrence Livermore National Laboratory, 7000 East Avenue, Livermore, California 94550, United States

This document contains Supplementary Information and figures describing complete set of experimental data and further discussion on energetic performance of our flow-between CDI (fbCDI) cell.

Contents

S.1.	Voltage profile under constant current conditions	2

S.2.	Effluent concentration measurement	3

S.3.	In-situ series resistance measurement	4

S.4.	Energy and cycle time measurements	6

S.5.	Energetic operational metric (EOM)	7

# Voltage profile under constant current conditions

As discussed in Section 2.3 of the main text, we performed a series of constant current charging/discharging experiments for a range of applied currents  and limit voltages . That is, we charged the cell with a constant current until the pre-determined limit voltage was reached. We then discharged the cell with the same current (with reversed direction) until the voltage reached zero. We present voltage profiles for 25-300 mA charging/discharging current () and 0.2-1.2 V limit voltage  in Fig. S.1. Each subplot shows the external voltage measurements for a fixed current  and different  values. Each profile is an overlay of 2 to 4 successive cycles under dynamic steady state (DSS) condition (to show cycle-to-cycle reproducibility). As mentioned in the main paper, the DSS condition is the operation mode wherein voltage and effluent concentration profiles vary negligibly between cycles; DSS is reached after a few cycles. We observe that this is indeed the case for the results in Fig. S1, as the voltage profiles shown here are very repeatable across cycles.

Fig. S.1. Measured external voltage versus time for 25-300 mA charging/discharging current () and limit voltages 0.2-1.2 V (). Galvanostatic voltage increases until the pre-set limit voltage is reached and current is reversed.  The jumps just after current reversals are associated with the fast response associated with purely serial resistive response.  Profiles shown here are all under DSS condition and each profile is an overlay of 2 to 4 successive cycles.

# Effluent concentration measurement

We measured effluent salt concentration via a calibrated in-line conductivity meter. To this end, we created a calibration curve relating the known KCl solution concentrations to measured conductivity. In Fig. S.2, we present effluent concentration versus time for experimental conditions identical to those of Fig. S.1. Flow rate was held constant at 2 . Dashed lines in each subplot show the influent concentration level. Each curve is an overlay of 2 to 4 cycles under DSS condition. Results show very good cycle-to-cycle repeatability for effluent concentration. In Fig. S.3, we show example measured cell voltage and effluent concentration for the case of 200 mA current and 0.8 V maximum external potential from startup until six cycles. Results show establishment of DSS condition after first few cycles.

Fig. S.2. Raw measurements of effluent concentration profiles measured via an in-line conductivity meter. Each curve is an overlay of two or more cycles under DSS condition. Dashed lines show influent concentration level.

Fig. S.3. Measured (a) voltage and (b) effluent concentration for  and  during the first six cycles. DSS condition is established after first few cycles.

# In-situ series resistance measurement

In Section 3.2 of the main text, we briefly introduced the procedure for in-situ series resistance measurement. We here discuss this process in more detail. As mentioned in Section 3.2 of the main paper, we provide galvanostatic control of the cell at specified currents (and pre-set voltage limits) using a sourcemeter (Keithley 2400, Cleveland, OH).  We then use the same sourcemeter to probe the CDI cell in real-time to measure its serial resistance response. As mentioned in the main text, we use the strong disparity in time response between series and non-series resistances to real-time sample series resistance component of CDI cells. Namely, we apply a small-amplitude (2 mA) AC current signal with ~10 Hz frequency during small portion of the charging or discharging current steps (within each charging or discharging half-cycle we apply a DC current ). We apply this 10 Hz probing signal once the external voltage is a multiple of 50 mV (e.g. at 0.4, 0.45, 0.5 V, etc.) and sustain this for order 1 s durations at a time. We initiate such pulse modulated AC currents roughly every 15 s to 4 min during charging and discharging (which last order 4 to 90 min, depending on applied current and set voltage limit). In Figs. S.4a and S.4b, we show example of applied current and corresponding voltage response signals for the case of 200 mA, 1 V, and 1 V during a typical charging step. The applied current profile is a saw-tooth signal with a mean value of  and peak-to-peak amplitude  of 2 mA. Voltage is a saw-tooth signal on top of an underlying approximately linear voltage response. The DC current signal () is responsible for charging/discharging the cell and the linear feature in voltage signal. As a result, this underlying voltage feature should be subtracted from the measured signal for correct resistance measurement. We label the voltage signal amplitude about this linear trend as  in Fig. S.4b. Series resistance of the cell can then be calculated simply by the ratio of  to  ().

Fig. S.5 shows the results of resistance measurement versus time with the method discussed above for experimental conditions similar to those of Fig. S.1. Each curve is an overlay of 2 to 4 cycles under DSS condition. In Fig. S.6, we present the same resistance data but here plot them as a function of . Both figures show higher (lower) series resistance during charging (discharging), consistent with the respective depletion (enrichment) of ions from (into) the spacer layer. Also, variation of resistance is greater at higher currents as expected.

Fig. S.4. (a) An example of 2 mA amplitude AC current probe signal () with a fixed 200 mA DC component () used for in-situ resistance measurement of our fbCDI cell. (b) Voltage response of the cell for current signal shown in (a). The response consists of saw-tooth with the underlying linear component associated with the charging of electrodes. To calculate resistance, we subtract the underlying linear signal variation from voltage response and divide the amplitude of resulting signal () by.

Fig. S.5. Time resolved series resistance for various currents (25-300 mA) and limit voltages (0.2-1.2 V) during cell operation. Each curve is an overlay of resistance measurements for 2 to 4 cycles under DSS condition.

Fig. S.6. Series resistance during cell operation as a function of  for various currents (25-300 mA) and limit voltages (0.2-1.2 V). Resistance values form a closed loop for each experimental condition. The loop becomes wider and more asymmetric under higher currents and higher , which we attribute to the effect of depletion and enrichment of ions from the spacer region (substantial salt removal and enrichment during charging and discharging, respectively).

# Energy and cycle time measurements

As discussed in Section 3.1 of the main text, we measured the input and output energy ( and ) of the cell operation under a variety of current and voltage conditions by integrating measured instantaneous power over the charging and discharging phases. We present the results as a function of  in Figs. S.7a and S.7b. Both  and  monotonically increase with . In contrast, current magnitude has a competing effect on input and output energies. Fig. S.7a shows that energy input  is generally greater when the cell is operated at higher currents (see arrow in Fig. S.7a). Energy recovered , however, decreases as discharge current magnitude increases. This leads to greater energy loss () at high currents, as shown in Fig. 4a of the main text. We additionally plot the cycle time (in units of min) versus  in Fig. S.7c. This figure shows an approximately linear relation between cycle time  and

Fig. S.7. (a) Input and (b) recovered electrical energy of our fbCDI cell as a function of  for currents in the range of 25-300 mA. Both energies increase monotonically with , but current magnitude has opposite effects on input and recovered energy (see arrows in (a) and (b)). (c) Cycle time versus  under experimental conditions similar to those of (a) and (b). Cycle time and  are approximately linearly dependent.

# Energetic operational metric (EOM)

To study the combined effect of ENAS and ASAR on desalination performance, we introduce an energetic operational metric (EOM) as the product of average salt adsorption rate (ASAR) and energy-normalized adsorbed salt (ENAS). We stress that this EOM is just one arbitrary “cost function”, which we use here as an example global optimization used to balance the trade-off between desalination throughput and energy efficiency. Other possibilities include a monomial form  or linear form  where  and  are arbitrary positive constants determined by the user and which reflect the relative value the user places on adsorption rate versus energy loss. The EOM we present here () is one example figure of merit describing global performance. We then seek a combination of current and  (or equivalently, current and cycling time) to maximize our EOM. Fig. S.8 shows an interpolated contour plot of the EOM as a function of  and external current. The markers overlaid on the contour plot are the corresponding measurement points (similar to those in Fig. 7 in main text). The dashed curve is the locus of operational points where resistive loss equals parasitic loss. Fig. S.8 shows that the EOM dramatically decreases in the limit of low current and high  (dominant parasitic loss, negligible ASAR) as well as high current, low  (dominant resistive loss, negligible ENAS). EOM, on the other hand, is maximized at moderate values of current and . The location of maximum EOM coincides with comparable resistive and parasitic losses.

Fig. S.8. Contour plot of EOM (defined as ) as a function of current  and . Dashed curve and the associated “parasitic dominant” shaded region are consistent with Fig. 7 of the main text. As with our earlier observations, EOM is maximized roughly in the regions with comparable resistive and parasitic losses.

To whom correspondence should be addressed. Tel. 650-736-1283, Fax 650-723-7657, E-mail: juan.santiago@stanford.edu